****

**“EASCO” CI Ball Float Steam Trap Flanged**

****

|  |  |  |  |
| --- | --- | --- | --- |
| **No.** | **Description** | **Material** | **Qty** |
| 1 | Cover Flange | ASTM A48 CL300 | 1 |
| 2 | Body | ASTM A48 CL300 | 1 |
| 3 | Pivot Frame | SS304 | 1 |
| 4 | Support Frame | SS304 | 1 |
| 5 | Valve Seat | SS410 | 1 |
| 6 | Pivot Pin | SS304 | 1 |
| 7 | Set Screw | SS304 | 2 |
| 8 | SLR Housing | SS410 | 1 |
| 9 | SLR Plug | SS410 | 1 |
| 10 | Ball Float With Lever | SS304 | 1 |
| 11 | SLR Pin | SS304 | 1 |
| 12 | SLR Seat | SS410 | 1 |
| 13 | Cover Bolt | Steel | 4 |
| 14 | SLR Gasket | SS304 | 1 |
| 15 | Valve Seat Gasket | SS304 | 1 |
| 16 | Cover Gasket | Comp. Non Asb. | 1 |
| 17 | Valve | SS304 | 1 |

**Limiting Conditions:-**

**Size: 25mm Flanged**

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **End Connection** | **Flange OD D mm** | **Total Thickness T mm** | **Working Pr. (Max) Kg/cm2** | **Working Temp (T)** | **Test Pr. (Max) Kg/cm2** |
| PN 16 | 115 | 16 | 14 | 426 C | 28 |
| ASA 150 | 108 | 17.5 | 14.22 | 426 C | 28 |

**Due to continuous development Program, the design & data given in this leaflet are subject to change without prior notice.**

**ANITA ENGINEERING WORKS**



58-59, Narayan Estate, Opp. Shree Ram Estate, Nr. CMC Ltd. Odhav, Ahmedabad-382415, Gujarat, India

Phone: +91 79 22974101, Fax: +91 79 22875014

Email: eascovalves@gmail.com, eascovalves@yahoo.com, Web: [www.eascovalve.com](http://www.eascovalve.com)